Appendix №3 to the Procurement Organization and Implementation Policy of Kumtor Gold Company CJSC

APPROVED BY:

Full name _____________________

KGC Deputy Chairman of the Board

_________________________, 2025

Terms of Reference for the purchase of 15 mm diameter steel grinding balls, increased surface hardness group 3, for Kumtor Gold Company CJSC

| Item № | Requirement parameters for goods, works, services to be purchased (subject of the purchase) | ### Designation Notes: - 15 mm diameter steel grinding balls, increased surface hardness group 3, GOST 7524-2015. |
| --- | --- | --- |
| 1 | Name/type/quantity/volumes/measure unit | ### 15 mm grinding balls, group 3, GOST 7524-2015. ### 1,601,700 kg |
| 2 | Delivery Location | ### For non-residents: - DAP- 9 Naryn highway, Balykchy, Kyrgyz Republic, Station code 717703. ### For residents: - Price 1: DAP- 9 Naryn highway, Balykchy, Kyrgyz Republic, Station code 717703. - Price 2: DAP - Kumtor Mine. |
| 3 | Delivery Deadline | ### Deadline will be determined after the agreement has been concluded. |
| 4 | Requirements for goods, services and works to be delivered | ### 4.1 Basic characteristics ### 4.1.1 Balls shall be manufactured in accordance with the requirements of GOST 7524-2015. 4.1.2 Ball dimensions and limit deviations are given in Table 1: In millimeters. Rated diameter; Nominal diameter; Limit deviations from the nominal diameter. 15; 15.0; ±1.0. 4.1.3 Ball hardness after heat treatment shall comply with the values specified in Table 2. Table 2 Rated ball diameter, mm; Ball hardness group. 1; 2; 3; 4; 5. Hardness, HRC/HB, not less. ball surface; at a depth of 0.5 ball radius; ball surface; volumetric. From 15 to 45 inclusive; 45/415; 49/461; 55/534; 55/534; 45/415; 61/601; 57/555. Notes: 1. Ball volumetric hardness value is optional. 2. By agreement of the manufacturer with the consumer, it is allowed to specify the upper limit of ball hardness. 3. The manufacturer and consumer shall use one method of determining ball hardness.. 4.1.4 Balls shall be made of steel, in which the carbon content and carbon equivalent shall correspond to the values given in Table 3. Table 3 Rated ball diameter, mm; Ball hardness group; Carbon mass fraction; Carbon equivalent. %, not less than. From 15 to 55 inclusive; 1.2; 0.40; 0.50. 3; 0.60; 0.70. 4.5; 0.75. 4.1.5 Cracks and defects on the ball surface, which take the ball dimensions beyond the limit deviations, shall not be allowed. 4.2 Marking 4.2.1 Balls shall not be marked. 4.2.2 Transport marking shall be in accordance with GOST 14192. 4.3 Packaging 4.3.1. 15 mm diameter balls shall be delivered in 1 (one) ton big bags.. |
| 5 | Acceptance procedure | The Supplier shall be responsible for: - Proper quality that meets all parameters specified in the certificate of conformity. - Timely delivery. - Reimbursement at its own expense if any defects are identified during the warranty period. Ensuring complete safety of the Goods from any kind of damage during all types of transportation to the Buyer's warehouse. Balls shall be accepted and delivered in batches. The batch to be tested shall consist of balls of the same size, of the same hardness group. The batch shall be accompanied by a quality document, which contains, among other things: - manufacturer's name; - product designation; - batch number; - weight of the shipped batch; - ball hardness test results; - stamp of the product quality control service. |
| 6 | Transportation and storage | Balls shall be transported by all types of transport in accordance with the applicable cargo transportation rules. Balls of different sizes and hardness groups shall not be mixed during transportation. |
| 7 | Warranty Obligations | The TOR data shall be confidential. The Contractor shall be liable for disclosure to third parties. |
| 8 | Test batch | If a supplier who has not previously supplied this type of product to KGC successfully passes the qualification and technical selection process, the Buyer shall have the right to initiate the conclusion of a supply agreement for a pilot (test) batch of products. The volume of the test supply shall be determined based on the average weekly consumption of the relevant product, calculated from actual operational data. After the test samples of the products have passed or failed the test, the purchase initiator shall provide an appropriate document on the test results, confirming the suitability or unsuitability of the products for production. The product shall be tested at the Kumtor Mine Mill, with the supplier’s representative required to be present. The price of the test batch shall not exceed the price specified in the commercial proposal. |

Drafted by: _________________________________________________________________

Full Name                                 Signature                                  Date

Agreed with: _______________________________________________________________

Full Name                                 Signature                                  Date