03.01.008

PIPE 16" SCH. 40/.375 INCH STANDARD WALL THICKNESS, NATURAL RUBBERLINED, VICTAULIC GROOVED, 10 FOOT LENGTH

• PIPE MATERIAL: CARBON STEEL ( ASME B36.1M)

• OUTSIDE DIAMETER: 406.4 MM

• WALL THICKNESS: 9.53 MM

• INTERNAL LINING: NATURAL RUBBER, 6 MM THICK,  VULCANIZED

• HARDNESS 40 ± 5 SHORE A,

• END CONNECTION: GROOVED (VICTAULIC ) SPECIFICATION 25.01,

• LENGTH: 10 FT (3.05 M)