Спецификация на кабель 50.15.112 (или аналог)
Specification for cable 50.15.112 (or alternative cable)
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Specification:
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3/C CU 8KV Type SHD-GC RHINOSHIELD™ CPE Mining Cable 90°C.
MSHA Approved

Fexible Copperconductors, EPR 100% Insulation Leve, Cu/Nylon Brid Shied, Exva Heavy Dy Two Layer Chioinated
Polythylane (CPE) Jacket with Optional Refetive Stipes
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nago ot oscdle. S Table 1 for Gmersions.

CONSTRUCTION:

1. Conductor: i coated, soft drawn, annealed, flexbl, apeday sranded copper per ASTM B33 and 8172

‘Separator Tape: Semi-conducting tape appled between the conductor and insulation 1 fciftte stiping

Conductor Shield: Semi-conducting cros-inke copolymer

Insulation: Eihylene Propylene Aubber (EPR)

Insulation Shield: Sippable s <conduetng crossinked copolymer

Braid Shield: i coated, soft e, annealed, coppr braid shiel (60% minimum coveragl, combined with color

coded nylon Blac, B, R o Black, Whit, Red] with a 40% maximum coverage

7. Ground Conductor: Two uninsulate, tncoate, soft chann, amneald, ope sranded, fleibl laycopper e ASTM
B33 and 8172

8. Ground Check Conducto: incoated, sftcrawn, annealed, ope sranded, fleibe ly copper er ASTM B33 and
8172 with high strength velow, poypropylene insulation

9. Fillr:Aubber filrs s neede

10. Reinforcement Reinfrcing twine applied over core

11, Inmer Jacket: Black, mold cured, xta heavy oty integral i, flame resistan, thermoseting Chloinated Polyethylene.
(cpe)

12. Outer Jacket: Black, mold ure, extra heawyduty,flame reistant, themmoseting Chirinated Polethylene (CPE)
Altemate jacket colors avalable

13. Reflective Stripe: Highly visibla reflectiv stipe embekded ino the outer jacke 0 incease safety and help pevent
cable runover [optiona, contac your ales representative for part number]
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« ASTM B33 Standard Specification for Tin-Coated Soft or Annealed Copper Wire

« ASTM B172 Standard Specification for Rope-Lay-Stranded Copper Conductors Having Bunch-Stranded Copper Conductors
« ICEA S-75-381 Portable and Power Feeder Cables for Use in Mines

 CSA Listed File # LLB5300 FT1, FT4, FT5 CSA C22.2, No. 96 Portable Power Cables

« MSHA listed: passes MSHA flame test

« Meets or exceeds ICEA requirements as applicable for ICEA S-75-381/NEMA WC 58, ASTM B-3




