Terms of Reference for the Purchase of Activated Carbon Reagent

| Item № | Required parameters for goods, work, services to be purchased (subject of the purchase) | For gold adsorption leaching and gold recovery from cyanide solutions. |
| --- | --- | --- |
| 1 | Name/type/quantity/volumes/measure unit | Coconut shell-based activated carbon for gold adsorption from cyanide solutions. |
| 2 | Delivery location | 9 Naryn Highway, Balykchy, Issyk-Kul Region. |
| 3 | Delivery deadline | Four months from the date of the order placement. |
| 4 | Procedure (sequence, stages) of work | The Supplier shall provide a Сommercial Proposal based on the specified activated carbon parameters and shall submit the product quality certificate. |
| 5 | Requirements for goods, services and work to be delivered | High-strength coconut shell-based activated carbon for gold adsorption from cyanide solutions. CAS № 7440-44-0. - Main physical and chemical characteristics: - Chemical formula: C. - Particle size distribution: 6×12 mesh. - pH ≤ 9-11. - Carbon Tetrachloride Activity (CTC activity): at least 55–60%. - Bulk density: 450-600 g/l. - Iodine number: not less than 1,050–1,100 mg/g. - Ignition temperature: not lower than 220°C. - Ash content: not more than 5%. - Humidity: not more than 5%. - Mechanical characteristics: - Hardness: not less than 95% according to GOST R 55873-2013, ASTM D3802-10 and GOST 16188-70. - Attrition resistance (Attrition number): according to ASTM D4058. - Fine fraction content (-12 mesh): not more than 5%. - Adsorption characteristics: - Intended for use in CIP/CIL processes. - High gold adsorption kinetics from cyanide solutions. - Gold loading capacity under production conditions: not less than 25 kg Au/t of carbon. - Operational requirements: The activated carbon shall maintain its mechanical strength, adsorption properties, and operational performance after multiple cycles of adsorption, desorption, and thermal regeneration. - Climatic conditions: The facility is located at an altitude of 4,000 m above sea level, where ambient temperatures may drop to -40°C. The product shall be resistant to extremely low temperatures and shall maintain its performance under severe conditions. |
| 6 | Requirements for the submission of technical and related documentation to the Client upon completion of the work | The Supplier shall provide the Client with: - COA (Certificate of Analysis)/Certificate of Quality. - MSDS/SDS (Material Safety Data Sheet). - Certificate of Origin of Raw Material. - Laboratory Test Report confirming compliance with all specified parameters. Packaging requirements: - The activated carbon shall be supplied Big Bags. One pallet shall contain two bags, 900–1,100 kg each, equipped with a moisture-resistant liner. - The Supplier shall provide a sample for laboratory testing. |
| 7 | Warranty obligations | The warranty period shall be at least 12 months from the date of delivery, subject to compliance with the recommended storage conditions. |